Packaging specification: 14

Basic Protective Packaging with Plastic for Tinplate Sheets

Code 14: Basic protective packaging for Vanderbijlpark Tinplate sheets

- Steel Strapping Seal

- 19mm Steel strapping

- Angle bracket

- Wooden pallet

- PVC plastic

I.	Information label

## Corrosion considerations

- Basic Protection is obtained by covering the material with PVC plastic.

- The packaging is not fully airtight and necessitates that coils be appropriately protected against rain and wetness during loading, transit and off-loading.

- To prevent condensation and sweating the coils must be stored in a dry, ventilated warehouse.

- The minimum number of days after receipt, before the onset of corrosion can be expected under correct storage conditions with undamaged packaging is indicated in the table below.

Corrosion guarantee

| Description | Product code | SPE | * Allowed claim period per surface treatment |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | None | Passivated | Dos oil | Rust preventative oil |
| Tinplate | TP, | 150 | n/a | n/a | 60 | n/a |

* Days after receipt of material.

n/a- not available.

Note

- Claims for corrosion will only be considered by ArcelorMittal South Africa if the material has been properly stored in a dry, ventilated warehouse, and the claims submitted within the periods indicated above.

- Once protective packaging has been removed and material taken into stock, ArcelorMittal South Africa will not consider any claims for corrosion.

- Material should be off-loaded under cover and not in the open.