Packaging specification: 47

Basic Protective Packaging with VCI Plastic for Tinplate  Coils vertically packed on steel pallet

Code 47: Basic protective packaging with VCI plastic for Tinplate coils

I.    Information labels

- VCI Plastic bag 120 micron

- Steel strapping seal

- Corner bracket polypropylene

- Steel strapping 32 x 0.8mm to secure coil on steel pallet

- Protection layer pad under the coil

- Steel pallet

- Reinforced PE-coated VCI paper (Food Grade) covering the coil

- Nylon strap to secure plastic bag at bottom of coil

Corrosion considerations

- Basic Protection is obtained by covering the material with VCI plastic.

- The packaging is not fully airtight and necessitates that coils be appropriately protected against rain and wetness during loading, transit and off-loading.

- To prevent condensation and sweating the coils must be stored in a dry, ventilated warehouse.

- The minimum number of days after receipt before the onset of corrosion can be expected, under correct storage conditions and undamaged packaging is indicated below.

Corrosion guarantee

| Description | Product code | SPE | * Allowed claim period per surface treatment |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | None | Passivated | Dos oil | Rust preventative oil |
| Tinplate | TPC | 150 | n/a | n/a | 180 | n/a |

* Days after receipt of material.

n/a- not available/applicable

Note:

- Claims for corrosion will only be considered by ArcelorMittal South Africa if the material has been properly stored in a dry, ventilated warehouse, and the claims submitted within the periods indicated above.

- Once protective packaging has been removed and material taken into stock, ArcelorMittal South Africa will not consider any claims for corrosion.

- Coils should be off-loaded under cover and not in the open.

- Arrangements must be made with ArcelorMittal South Africa regarding the return of pallets and inner sleeves.