Packaging specification: 50

Advanced Protective Packaging with Rust Preventive and Reinforced Paper for Tin & DWI Coils (export)

Code 50: Vertically Packed on Wooden Pallet. Packing for sensitive material.

Advanced protective packing with rust preventative and reinforced paper for

Tin & DWI Coils (export).

1.	Notes:	INTERMEDIATE STAGE:

1.	Low tack tape

2.	Reinforced PE coated VCI paper (Bottom end)

3.	Bottom cover galv. plate

4.	Bottom galv. corner bracket

5.	Wooden pallet

6.	Reinforced PE coated VCI paper (Coil wrap around, pressed into eye)

7.	Tape (Sealing off PE coated VCI paper)

8.	Cardboard (Coil wrap around)

Notes:	FINAL STAGE:

9.	Galv. Sheet (Belly plate)

10.	Reinforced PE coated VCI paper (Top end)

11.	Top cover lid

12.	Top galv. Rippled corner plate

13.	Strapping (Corner plate and belly plate)

14.	Duct tape (Seal overlapping belly plate)

15. Card board protection strip

16.	Strap seal

17.	Wooden blocks on pallet

18.	High tensile strapping

19.	Shore wood

P.	Packaging label		NOTE:

1.	VCI Paper to be food-

stuff compatible

I.	Information label		2.	Desiccant bag in eye of coil (1kg)

Corrosion considerations

	Packaging classified as Advanced Protective with enhanced corrosion protection. This is achieved through the incorporation of a rust preventative paper/plastic together with a cover sheet.

	Although advanced, the packaging is not fully airtight which implies that coils must be appropriately protected against rain and moisture during loading, transit and off-loading.

	To prevent condensation and premature deterioration of strip surface condition, the coils must be stored in a dry, ventilated warehouse.

	The minimum number of days after receipt before which the onset of corrosion can be expected for the packaging method under correct storage conditions and with undamaged packaging are indicated in the following table.

Corrosion guarantee

| DESCRIPTION | PRODUCT CODE | SPE | * CLAIM ALLOW PERIOD PER SURFACE TREATMENT |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | None | Passivated | Dos oil | Rust preventative oil |
| Black Plate Coils, Prime (Export) | TPCB | 156 | 0 | n/a | n/a | n/a |
| Tinplate | TPC | 150 | n/a | n/a | 90 | n/a |
| Tinplate DWI | ITC | 155 | n/a | n/a | 90 | n/a |

* Days after receipt of material.

n/a- not available/applicable

Note:

	Coils must be off-loaded under cover and not in the open.

	Claims for corrosion will only be considered by Mittal Steel South Africa if the material has been properly stored in a dry, ventilated warehouse, and the claims submitted within the periods indicated above,

	Once protective packaging has been removed and material taken into stock, Mittal Steel South Africa will not consider any claims for corrosion.