Packaging specification: 51

Basic Protective Packaging with VCI Plastic for Tin Plate Coils vertically packed on plastic pallet

Code 51: Basic protective packaging with VCI plastic for Tin plate coils

I.	Information label

- VCI Plastic bag 150 micron

- Steel strapping 32 x 0.8mm around plastic pallet to secure pallet around base of coil

- Steel strapping seal

- Plastic pallet (Type D for small coils; Type E for large coils)

- Reinforced PE-coated VCI paper (Food Grade) covering the coil

- Nylon strap to secure plastic bag at the bottom of the plastic pallet

Corrosion considerations

- Basic Protection is obtained by covering the material with VCI plastic.

- The packaging is not fully airtight and necessitates that coils be appropriately protected against rain and wetness during loading, transit and off-loading.

- To prevent condensation and sweating the coils must be stored in a dry, ventilated warehouse.

- The minimum number of days after receipt before the onset of corrosion can be expected, under correct storage conditions and undamaged packaging is indicated below.

Corrosion guarantee

| Description | Product code | Price List (SPE) | * Allowed claim period per surface treatment |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | None | Passivated | DOS oil | Rust preventative oil |
| Tinplate | TPC | 150 | N /A | N /A | 180 | N/A |

* Days after receipt of material.

N/A- not available/applicable

Note:

- Claims for corrosion will only be considered by ArcelorMittal South Africa if the material has been properly stored in a dry, ventilated warehouse, and the claims submitted within the periods indicated above.

- Once protective packaging has been removed and material taken into stock, ArcelorMittal South Africa will not consider any claims for corrosion.

- Coils should be off-loaded under cover and not in the open.

- Arrangements must be made with ArcelorMittal South Africa regarding the return of pallets and inner sleeves.